## Slide 1: The Need for Self-Assembly
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Earlier we discussed Microfabrication:
A method for simultaneously making large numbers of IC / MEMS devices
It's very efficient and very cost-effective . . .
But use of projected light images → Sizes > λlight (deep UV ~ 0.05 micron)
In our last class I described methods of making things MUCH smaller
Atomic Force Microscope writing oxide patterns or melting polymer pits
Scanning Tunneling Microscopes pushing atoms . . .
Electron Beams patterning photographic emulsions
But new techniques often fell on wrong side of science vs. technology boundary
Key figure (introduced in lecture 5) was:

## Slide 2: Processing rate vs. lithography and its best resolution
Source: Don Tennant of Bell Labs
- 25 Hours
Photolithography
E-beam lithography
- 3000 Years
- 3 billion years
AFM lithography
STM lithography
- 30 Years
- 1/100 seconds
Processing time for 5x5 mm2
1/10,000 the area single Si wafer

## Slide 3: Producing a dilemma:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Microfabrication: Efficient but crude (on the nanoscale)
Nanofabrication using AFM or STM: Precise, but lifetime of universe to pattern one wafer
These are now often described as "Top Down Fabrication" techniques
TOP DOWN in that we 109 X larger humans are trying to directly control everything
That is, top down in a management sense
TOP DOWN in that we often start with LARGE things and try to whittle them smaller
E.G. microfabrication's deposition of whole layers → etch away unwanted portions
Alternative? "Bottom Up Fabrication"

## Slide 4: Bottom Up Fabrication
1) START with nanoscale things
Researchers have made a LOT of progress with this
2) Then try to find a way to get them organized in useful ways
But here we are still on a steep leaning curve!
Focusing on the second more difficult step, this bottom up process is also called:
SELF - ASSEMBLY
(That is: Figure out a way to get mother nature to do the hard part)
Nanoscale self-assembly has been going on for BILLIONS of years
Challenges are to figure: WHERE it has been going on (we can't SEE it directly)
Which forms of self-assembly might be useful

## Slide 5: SELF-ASSEMBLY (most often) = Lower energy through organization
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
1) Trivial case – only one possible end state:
Start: Finish:
2) More realistic – many possible end states (but one slightly favored):
Start: Finish:

## Slide 6: Or helped by catalysts and enzymes ("Semi Self-Assembly?")
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
3) CATALYSTS: GUIDE parts toward final LOWER ENERGY state:
Start:
Finish:
Intermediate:
4) ENZYMES: DRIVE pieces to state that may even be at HIGHER ENERGY
Using force/energy provided by enzyme (e.g., fueled by ATP → ADP)
As occurs with many forms of DNA and protein "self-assembly"

## Slide 7: Looking more deeply:
Say that we want to "grow" (i.e. self-assemble) more of the structure at the left:
New piece arrives at more weakly bound position
This takes more time, especially because jump DIRECTION is likely RANDOM:
SO new piece actually wanders about until it STUMBLES upon "perfect" point
Ideally, new piece arrives at "perfect" multi-bonding attachment point
More complicated (but realistic) scenario:
Then jumps until it
reaches "perfect" point

## Slide 8: Sounds like that might take a heck of a long time!
** Reference: https://courses.cit.cornell.edu/ece407/Lectures/handout21.pdf
What it actually takes is a whole lot of jumps (for wandering to finally pay off)
So elapsed time depends on time per jump (or jump frequency)
Relevant quantity is atomic vibration frequency = "Debeye Frequency"
Because some fraction of vibrations ( ) produce jumps ( )
But Debeye frequencies are HUGE:
For Silicon (at ~ 400°C)** ~ 2-20 THz (i.e. 2-20 x 1012 times per second)
Debeye vibrational frequencies are even HUGE at 25°C !
AS TEMPERATURE INCREASES: Vibrational frequency AND amplitude increase
becomes = increasing jumps
Implying, instead, that self-assembly could progress VERY rapidly!

## Slide 9: But there are other potential problems:
What happens if a second piece arrives too soon?
Self-assembly is getting into big trouble:
First piece is now buried, no longer independent, semi-locked into (wrong) position!
First piece alights between "atoms"
Given a short bit of time it would wiggle over to full bonding position
But before that can occur,
second piece arrives to sit atop it

## Slide 10: SELF-ASSEMBLY STRATEGY #1:
SLOW DOWN, reducing arrival rates, giving each new piece time to settle in
How do you "reduce arrival rates?"
- In self-assembly from solution, reduce concentration of reactants
- In self-assembly from gas, reduce partial pressures of reactants
TURN UP THE TEMPERATURE, so that things "settle in" faster
Because vibrations and jumps will then all happen more quickly
It's like doing everything in "fast forward"
SELF-ASSEMBLY STRATEGY #2:

## Slide 11: Another Oops: Piece that is accommodated in alternative arrangement
What we'd expected (or hoped for): But at only slightly higher energy (nearly as likely):
Leading to assembly we'd hoped for:
Or something VERY different:

## Slide 12: Key to dealing with this is exploitation of REVERSIBILITY
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Temperature driven vibrations and jumps continuously . . .
ARRANGE AND REARRANGE:
ASSEMBLE AND DISASSEMBLE:
OR:

## Slide 13: So things that are "done" are also being continuously "undone"
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
But lower energy configurations are "undone" less frequently / readily (they're more stable!)
IDEAL would be sudden loss of stability with increasing temperature:
TEMPERATURE
STABLITY OF #1
STABLITY of #2
T1
T2
SWEET SPOT
T1 < T < T2
ONLY #2 Stable

## Slide 14: Unfortunately things are not quite that simple
Generally, regions of stability and instability do not have sharp temperature boundaries
That can be played against each other to promote certain structures
Stability is instead PROBABILISTIC, governed by "Arrhenius" / "Boltzmann" / "Fermi" behavior:
That is, involving factors like: e – E1 / k T
Yielding probability plots of stability similar to this (for E2 > E1):
Temperature
100%
SELF-ASSEMBLY STRATEGY #3: Stay in SWEET-ish Zone
(where Prob #2 >> Prob #1)
Probability that #2 is stable
Probability that #1 is stable

## Slide 15: And then there are impurities to deal with:
"Impurity" = anything else you really hadn't planned on being present:
OR:
Disrupted structure:
Whole new structure:
SELF-ASSEMBLY STRATEGY #4: Get rid of almost all impurities
Sometimes possible with self-assembly from gas (i.e., some forms of crystal growth)
Hopeless with aqueous growth (i.e., chemistry, where must later refine out mistakes)
SELF-ASSEMBLY STRATEGY #5: Again try to find a "SWEET-ish" temperature zone
But this time where only impurity bonding becomes unstable

## Slide 16: TIME FOR SOME EXAMPLES: Crystal growth of glass microspheres
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Source: Interdisciplinary Education Group, NSF MRSEC project of the University of Wisconsin.
http://www.mrsec.wisc.edu/Edetc/cineplex/self/text.html
Supporting webpage with embedded animation:
The Need for Self-Assembly - Supporting Materials - Animation_1

## Slide 17: That was a less than perfect example of self-assembly:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
In semiconductor crystals, fewer than 1 in 1012 atoms can be out of place!!
So what was the problem with above crystal growth?
New atoms arrived way TOO quickly
Allowing no time for: Crystal to expel impurity atoms
Or to try to repair flawed crystal
In this case obvious solution = Turn down flux / Dilute concentration of reactants
With MANY faults in the crystal (involving 0.1 to 1% of “atoms”):
Faults
Impurities

## Slide 18: Another visualization of self-assembly: floating magnetized shapes
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Note how it takes many tries to find the ideal / lowest-energy configuration
Facilitated by agitation (background energy) to knock it out of less desirable states
Source: Interdisciplinary Education Group, NSF MRSEC project of the University of Wisconsin.
http://www.mrsec.wisc.edu/Edetc/cineplex/self/text.html
Crystal growth / self-assembly of floating plastic magnets:
Supporting webpage with embedded animation:
The Need for Self-Assembly - Supporting Materials - Animation_2

## Slide 19: But this time we didn’t get much overall crystal growth!
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Problem? Too much energy
Triangles briefly condensed - but then jumped back off
But this DID have side advantage: It grew almost no “Bad” mis-bonded crystal
Mis-bonded atoms were held so weakly that they re-evaporated VERY fast
Solution for this: Slow things down = Reduce temperature of the system

## Slide 20: Confirming earlier self-assembly strategies:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Best self-assembly almost always produced by a subtle optimization of temperature and flux:
Temperature:
Low temperatures: Easier to reach, less likely to liberate impurities from elsewhere,
and may best preserve desirable features of assembly
Moderate temperatures: Help newly arrived parts to quickly reach proper sites
High temperatures: Make it less likely that undesirable impurities will stick
or that more energetic arrangements will persist
Flux (or flow):
Higher the flux, faster the parts already on surface must get into proper positions
So higher fluxes require use of higher growth temperatures
But higher flux does make presence of ambient impurities less important
Because they then constitute smaller fraction of arriving parts (atoms)

## Slide 21: A neat example of naturally occurring self-assembly:
One that I only recently learned about!
Water, percolating down through rocks, leeches out (dissolves) silica (SiO2)
If the water then begins to dry up
Silica becomes supersaturated, and precipitates back out of solution
Under the right conditions, silica precipitates form uniform spheres, 100's of nm in diameter
If drying/precipitation is slow enough, spheres have time to get organized
First into sheets: And, eventually, into full 3D structures:

## Slide 22: When 3D regions grow into one another, you get the gemstone OPAL!
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Which is treasured for its "iridescent colors" (= colors that shift with viewing angle)
All because of Wave Diffraction!
Spheres are about the size of light's wavelength so they scatter light
Which adds constructively for one color (wavelength), in one direction
Or adds constructively for another color (wavelength), in another direction

## Slide 23: In the lab, I did something similar with individual atoms via: "Molecular Beam Epitaxy" (MBE)
Throw individual atoms across vacuum chamber (by evaporating them)
Let them land on mildly heated substrate (which allows them to still move around)
Arriving atoms ➔
<= Migrating atoms
But it takes 1M$ plus worth of vacuum equipment to make it this "simple"
My homepage view: My full two growth chamber system:
Arrow marks point where photo at left was taken

## Slide 24: OK, but where's the beef nano?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Sure, "MBE" involves nano atoms, but how does this produce nano structures?
Flip upside down, install TWO evaporation sources, then alternate atoms:
Viola!
Single atom layers!

## Slide 25: Or more realistically:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
From WeCanFigureThisOut.org: https://WeCanFigureThisOut.org/VL/MBE.htm
Supporting webpage with embedded animation:
The Need for Self-Assembly - Supporting Materials - Animation_3

## Slide 26: But what if you want 3D nano-structures?
1 Strained Layer Epitaxy of Germanium-Silicon Alloys, John C. Bean,
Invited Review, Science Magazine 230, 127-131 (1985)
Try with atoms of different sizes: Smaller Si atoms and larger Ge atoms
Alternative #1: Larger Ge atoms squeeze to fit = Strained Layer Epitaxy 1
Alternative #2: Arriving atoms exploit their surface mobility to segregate / island:
Favored at lower temperatures
Favored at higher temperatures

## Slide 27: Really do get such spontaneous 2D self assembly:
AFM image of slightly organized MBE Germanium islands on Silicon
(Stress-Induced Self-Organization of Nanoscale Structures in SiGe/Si Multilayer Films, C. Teichert, L.J. Peticolas, J.C. Bean, J. Tersoff and M.G. Lagally, Physical Review B 53 (24), 16334-7, 1996)
TEM cross-section of MBE Germanium island embedded in Silicon
"Analysis of the 3D relationship of Ge quantum dots in a Si matrix using focused ion beam tomography" A.J. Kubis, T.E. Vandervelde, J.C. Bean, D. Dunn, R. Hull, Nanoparticles and Nanowire Building Blocks-Synthesis, Processing, Characterization and Theory. 2p. 411 (2004), Materials Res. Soc.

## Slide 28: And this led to an even more complex 3D self-assembly:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
TEM Cross-section of MANY layers of self organizing Ge dots embedded in Si:
What you are seeing is this:
Ge islands growing atop Ge islands, growing atop Ge islands . . . WHY?
"Analysis of the 3D relationship of Ge quantum dots in a Si matrix using focused ion beam tomography" A.J. Kubis, T.E. Vandervelde, J.C. Bean, D. Dunn, R. Hull, Nanoparticles and Nanowire Building Blocks-Synthesis, Processing, Characterization and Theory. 2p. 411 (2004), Materials Res. Soc.

## Slide 29: Explanation comes from variation of earlier figure:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Explanation first published in: Stress-Induced Self-Organization of Nanoscale Structures in SiGe/Si Multilayer Films, C. Teichert, L.J. Peticolas, J.C. Bean, J. Tersoff and M.G. Lagally, Physical Review B 53 (24), 16334-7, 1996
Bulging Ge island on Si:
Stretches Si layer deposited above it:
Attracting next layer of Ge atoms:
And so on and so on . . .

## Slide 30: Device-relevant forms of self-assembly?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Consider proposal for nanoscale Quantum Cellular Automata:
Square array of Q-dots
with affinity for electrons
So small & close (~30 nm) that charges repel
End up only holding two charges
Two alternate charging
patterns => Digital 1 and 0!
Which can be manipulated
by input signal on wire.
And charge configuration
will then propagate along
a "wire" of such QCA
elements!
(Source: WeCanFigureThisOut.org https://wecanfigurethisout.org/VL/QCA_cells.htm)
Supporting webpage with embedded animation:
The Need for Self-Assembly - Supporting Materials - Animations_4_6

## Slide 31: Self-assembled QCA’s could be used in digital logic gates:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
QCA Majority, AND, OR gate
QCA Inverter
QCA Binary Adder!
(Source: WeCanFigureThisOut.org https://wecanfigurethisout.org/VL/QCA_logic.htm)
I’ll explain how these digital devices work in my Nanoelectronics lecture
Today’s question is: Can we con mother nature into self-assembling QCA’s?
Well, we’ve made a good start:

## Slide 32: Self-assembled QCA dot like structures:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
AFM image of MBE grown GeSi “quantum fortresses”
Higher resolution top views of QF's grown under slightly different conditions:
P. Kumar, T.E. Vandervelde, T. Kobayashi, J.L.Gray, T. Pernell, J. A. Floro, R. Hull, J.C. Bean, Applied Physics Letters 83, 5205-7 (2003)
Self-assembled QCA?

## Slide 33: How on earth did you get nature to do this?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Supporting webpage with embedded animation:
The Need for Self-Assembly - Supporting Materials - Animations_10_12

## Slide 34: Other unique forms of crystal self-assembly?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Heat metal dot on Si until melts.
Immerse in vapors of SiH4.
Si dissolves into molten metal (forming eutectic)
Then precipitates
onto Si surface
Now switch from SiH4 to GeH4 vapor:

## Slide 35: Are you pulling our leg? No:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
U. Helsinki: www.micronova.fi/units/ntq/research/nanowires.php
Switch back and forth between gases:
Lorelle Mansfield -NIST:
http://www.nist.gov/public_affairs/techbeat/tb2006_0525.htm
Switch gases after metal removed:
Or do both!

## Slide 36: Or how about self-assembly of gold nano particles:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
From CytImmune Inc:
Supporting webpage with embedded animation:
The Need for Self-Assembly - Supporting Materials - CytImmune

## Slide 37: What exactly did he do?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Basic Process:
Put gold chloride (HAuCl4) into solution liberating Au+ ions
Added sodium citrate "reducing agent" that de-ionizes the gold: Au+ => Au
Some Au atoms then start to clump together into sub nanometer nuclei
Remaining Au atoms then pile on => almost uniform Au nanoparticles
Size = 5 to 100 nm depending on gold chloride to sodium citrate ratio
OR can controllably enlarge nanoparticles in second process:
Put above particles into fresh HAuCl4 solution (creating new supply of Au+ ions)
"Reduce" driving those ions to coat old nanoparticles, enlarging them

## Slide 38: Is self-assembly ALL about crystal growth?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
ABSOLUTELY NOT! In fact I am running out of crystal growth examples
There are more numerous and more powerful examples in the wet world
A small sampler (with much more to follow in subsequent lectures):
Consider the peculiar properties of water:
Oxygen wants electrons much more than hydrogen
So charge distribution in water is not uniform - Molecule is "polarized"
O
H
H

## Slide 39: Which means that water molecules like to organize (sort of):
"A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
As liquid water jostles about, molecules tend to place (+) hydrogens next to (-) oxygens on neighbor
Energy reduced as opposite charges snuggle closer
“HYDROGEN BONDING”
(When solidifies, REALLY gets organized - Why it expands)
Screwed up if big non-polarized molecules (e.g. oils) inserted into mix:
Oils hold water molecules apart So oil and water tend to segregate

## Slide 40: But what if add polarized end group to oil?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Or even better:
Long molecules organize:
Hydrophillic (water loving) ends aligned in same direction
Becomes the low energy interface with the water
Then water IS attracted to ends:

## Slide 41: Use in complex self-assembly?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Float layer of oily molecules on top of water bath
Move surface barrier inward to compress oil layer
Monitor surface tension by the pull on a sheet partially immersed in bath to sense when oils "self-assemble" side to side

## Slide 42: Its called "Langmuir-Blodgett" film growth:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Courtesy of Professor Arend-Jan Schouten, Laboratory of Polymer Chemistry, University of Groningen, The Netherlands: http://polchajs.fmns.rug.nl/files/jv/lb.html

## Slide 43: But there is an even better molecular arrangement!
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Organize oils with special polarized
ends so that they are tail to tail:
Called a "lipid bilayer" - Ring a bell?
Both sides of film are now "hydrophillic" so it's happy to be immersed in water:
(OK, so I got tired of orienting dozens of tiny water molecules!)

## Slide 44: Which gives . . . a cell membrane!
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Which is constructed out of exactly such a “lipid bilayer” layer
And does not actually involve atomic bonding BETWEEN the lipid molecules!
Source: The World of the Cell, W.M. Becker, J.B. Reece and M.F. Poenie, Benjamin/Cummings Publishing, 3rd edition, page 27

## Slide 45: But how does nature actually assemble such things?
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Demonstration of how a virus shell might assemble:
Uses plastic subunits with embedded magnets to simulate bonding
From the Molecular Graphics Laboratory of Professor Arthur J. Olson of the Scripps Institute
http://mgl.scripps.edu/projects/tangible_models/movies
Supporting webpage with embedded animation:
The Need for Self-Assembly - Supporting Materials - Animation_15

## Slide 46: Or via computer animation:
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
From the “Auto Cell Project”
Shows not only how molecular fragments might assemble, but how their assembled structure would then produce more of the ingredient fragments!
Supporting webpage with embedded animation:
The Need for Self-Assembly - Supporting Materials - Animations_16_19

## Slide 47: But there is much more than mere atomic/molecular self-assembly!
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
To really get into PROGRAMMED self-assembly we need to learn about:
Organic chemistry → DNA Replication → Et Cetera
Topics of lectures to follow!!

## Slide 48: Credits / Acknowledgements
A Hands-on Introduction to Nanoscience: WeCanFigureThisOut.org/NANO/Nano_home.htm
Funding for this class was obtained from the National Science Foundation (under their Nanoscience Undergraduate Education program).
This set of notes was authored by John C. Bean who also created all figures not explicitly credited above.
Copyright John C. Bean
(However, permission is granted for use by individual instructors in non-profit academic institutions)